## Slide 1: Effect of Heterogeneity on Catastrophic Rupture
F.J.Ke a, b , H.L. Lia, M.F.Xia a, c and Y.L.Bai a
  a State Key Laboratory for Non-linear Mechanics (LNM),
  Institute of Mechanics, Chinese Academy of Sciences, Beijing 100080, China
  b Department of Applied Physics, Beijing University of Aeronautics and Astronautics, Beijing 100083, China
c Department of Physics, Peking University, Beijing 100871, China
ACES Meeting, May 5-10, 2002, Maui,Hawaii

## Slide 2
Successful prediction (of earthquake)
depends greatly on the heterogeneity
of the area’s structure
------ Mogi

## Slide 3
Damage Localization Rupture
Damage accumulation  catastrophic rupture

## Slide 4: Content
1. Heterogeneous Elastic -Brittle Model
2. Event Series prior to Rupture in Heterogeneous Media in Mean Field Approximation
3. Effect of Surrounding, Size Effect and Stress Re-Distribution
4. Network Simulations
5. Concluding Remarks

## Slide 5: 1. Heterogeneous Elastic -Brittle Model
Unique elastic behaviour (E)
Mesoscopically heterogeneous Brittle Fracture Strength c
c follows Weibull distribution
m: Weibull Modulus

## Slide 6: Weibull Distribution of Mesoscopic Strength c
m=10
m=5
m=2
Brittle Fiber Ductile metal
m 2 - 4 20
Notes: I give you an example of Weibull distribution of the mesos-copic strength c . That is for m=2, to 5, to 10.
You can see, the larger the Weibull modules the sharper of the distribution. So, you get the idea how about heterogeneity in the medium.
And, give you some idea for some brittle-fabres , Weibull modules can range from 2 to 4. For ductile metals, Weibull modules will be about 20.

## Slide 7: Heterogeneous Elastic -Brittle Model
Relation between Load(N) and Displacement(mm)
of Sandstone, from Chinese Encyclopedia, Mechanics,
p.529
Elastic - brittle model
m = 3

## Slide 8: 2. Event Series prior to Rupture in Heterogeneous Media
Damage Localization (DL)
Maximum Stress (m, i.e. d/d=0)
Energy Release (ER and ERmax)
Surrounding and Size-effect
Stress Re-Distribution(SRD)
Catastrophic Rupture (d/d = -Ks)
Critical Sensitivity (S)

## Slide 9
m=5
Rupture dER/d
when k=1
Damage D()
localization


## Slide 10
m=5
Notes: Now, some network simulations. I show you some two dimensional simulations here. This figure and the followings are the results of network simulations. In our simulations we use a network of about 100*100. The heterogeneity of medium in the simulation is formulated by Weibull distribution, but the mesoscopic spatial heterogeneity by random distribution. As you can understand in our analytical model there is medium heterogeneity but no spatial distribution . But in network simulations, there are both. I mean both the heterogeneity in strength and the spatial distribution of stress. Both effects are included in simulations. Additionally, the simulations are carried out with displacement-controlled boundary condition, namely stiff surroundings.
This is the result for the medium with m=5. Please notice the damage pattern at the point of maximum stress. It is also hard to see any clue for rupture. Now we turn to sensitivity S.

## Slide 11: 3. Size-effect and Stress Re-Distribution 4. Network Simulations

## Slide 12
Energy Release and
Catastrophic Rupture (CR)
Surroundings
Km
Sample
Ks
-Km

## Slide 13: m  3.591 implies catastrophic rupture (CR) for k=Ks/Km=1
Catastrophic Rupture has a lower bound of Weibull modulus
mc = k * exp[( mc+1)/mc]
k = 1
mc = 3.59
Notes: What is that? The condition is here. when Weibull modulus greater than 3.59,
this implies, catastrophic rupture can occur.
This comes from the condition and this equation . For different stiffness of surroudings , you can evaluate different values of critical Weibull modulus for k=1, mc=3.59.

## Slide 14
Network Model vs. Mean Field Model
Weibull modulus: 2
With elastic surroundings

## Slide 15
Network Model vs. Mean Field Model
Weibull modulus: 5
With elastic surroundings
k=1
Notes: 111

## Slide 16
Shear

## Slide 17
Size of Elastic Surrounding
Stiffness: Ks  Km
Lm Surrounding
Ls Sample

## Slide 18
Different k
Weibull modulus: 5
Black dash: rigid, Blue dash dot: k=1, Red solid:k=2

## Slide 19
2-D simulation,
white: failed
red : high stress
(Courtesy of YU Huaizhong)
Stress Re-distribution
due to heterogeneity
and damage

## Slide 23: 5. Concluding Remarks
Effects on Catastrophic Rupture owing to
Surroundings
Size Effect
Stress Re-Distribution (SRD)
For accurate prediction of catastrophic rupture, there is a need of close look of the relationship between various effects and rupture.

## Slide 24
Thanks